## Slide 1
2pt and 4pt measurements taken together with voltage bias at 300K. Initial few data points removed as they showed capacitance current. Samples very sensitive to range and settings of 6430 and 2182A, that may account for difference in 4pt measurements.
Sample “Large Trapezoid” 7

## Slide 2
@400K
RSD = 3MΩ
R4pt1 = 890kΩ
R4pt2 = 430kΩ

## Slide 3
400K:
Notes: VvsB=(2.35307e-05+6.45263e-05)/2 = 0.0000440285
i=1*10-9;
t=30*10-9;
Rh=t*VvsB/I
R4pt(B=0) = 279578 Ohms
Volt_spacing = 30 nm
Width = 20 nm

## Slide 4
Sample “Parallelogram” 1
400K:
Notes: VvsB=(0.000262828+0.000206281)/2;
i=1*10-9;
t=30*10-9;
Rh=t*VvsB/I
R4pt(B=0) = 279578 Ohms
Volt_spacing = 30 nm
Width = 20 nm

## Slide 6
not working
Sample “Parallelogram” 2

## Slide 7
@400K
RSD = .23MΩ
R4pt2 = 890kΩ

## Slide 8
400.0 K: (red)
400.0 K: (purple)
,
Sample: Small trapezoid A
Current 1nA
r = r0exp[(T0/T)1/3]

## Slide 9
Hall voltage 100nA, 400K
400.0 K: (red)
400.0 K: (purple)
,
4pt magneto-resistance, two pairs of contacts
100nA, 400K

## Slide 10
Sample: Large trapezoid A
400.0 K: (red)
400.0 K: (purple)
,
r = r0exp[(T0/T)1/3]

## Slide 11
Sample: Large trapezoid B
400K, 100nA
400.0 K: (red)
400.0 K: (purple)
,
300.0 K: (purple)
,
300K, 1nA