## Slide 1
JR190815_04 In2Se3
2pt
4pt

## Slide 2
IV curves as Gate voltage -75V to 75V
IV curves as Gate voltage 75V to -75V
This is the expected behavior for semiconductors, this sample is what we expect. The 75V measurements were taken 300s apart but the current seems to have dropped for some reason between them. I don’t know if this means there is a time dependence to the loop.
4pt VI curves as Gate voltage 75V to -75V. Taken with the first graph. Vsd-biased
I think this is why most people don’t do semiconductor 4pt. This doesn’t say much outside Ohmic range.

## Slide 3
4K
50K
100K
150K
200K
250K
270K
300K
All Temp

## Slide 4
4K
10K
20K
30K
50K
60K
70K
80K
40K
90K
100K
150K
200K
250K
270K

## Slide 5
300K

## Slide 6
S
D
1
2
3
4
R12
RS1
300K
R12
RS1
100K
R12
RS1
270K
200K
R12
RS1
100K
R12
RS1

## Slide 7
S
D
1
2
3
4

## Slide 8
Cooling
Warming
VG = 75V, VSD = .1V
Ramped at 300K from -75V to 75V
Cooled from 300K
Ramped at 4K from -75V to 75V
Warmed from 4K

## Slide 9
Attempted hall