## Slide 1
JR190919_03, In2Se3
pre
post
pre
post
300K pre/post heating
VSD = .1V
VG = 75V, VSD = .1V
Heating was done for 1hour at 400K in high vacuum

## Slide 2
300K
270K
250K
200K
150K
100K
90K
80K
70K
60K
50K
40K
30K
20K
10K
4K

## Slide 3
Loop
Warm
Loop
Warm
Loop
Cool
Loop
Warming 4K->300K
and
cooling 300K->4K
Both plots show max loops at Vg = 75V with VSD = .1V
Left is 2pt, right 4pt
cooling current is so low resistance is not shown
Loop
Warm
Loop
Warm

## Slide 4
4K, SD = .1V, cooled at 0V
4K, SD = .1V, cooled at 75V
4K, SD = 1V, cooled at 75V

## Slide 5
300K
VSD = 1V
VSD = .1V

## Slide 6
300K
25V increments
from -75V to 75V
Increasing VG
Decreasing VG
Decreasing VG
Increasing VG

## Slide 7
-75V warm
0V warm
75V warm
75V cool
Labels on chart all refer to what the gate voltage was when cooled. All measurements were taken at VG = 75V.
The 75V (cooling/warming) was done with VSD = 1V, the 0V and -75V were done with VSD = .1V.
So even with less SD voltage the 0V and -75V cooling seems to conduct more
2pt
4pt
-75V warm
0V warm
75V warm
75V cool
-75V warm
0V warm
75V warm
75V cool