## Slide 1: β-InSe by Seng Huat (Sam) Lee

## Slide 2
Powdered XRD pattern of InSe matched with the ICDD database PDF card 00-034-1431, β-InSe space group 194.
However, there are two impurity peaks at 27.89(1) and 28.94(2).

## Slide 3
From the In-Se phase diagram, the possible impurity for the growth of InSe will be either In4Se3 and In6Se7.
Since the stronger reflected peak of In4Se3 are occurred at 28.92 and those two observed impurity peaks matched with In4Se3, it is clear evidence the secondary phase is In4Se3.
The PDF card for β-, γ-InSe, and In4Se3 are attached.